## Slide 1
Non-Newtonian Fluid Mechanics
(Part - V)
Mechanical Engineering Department,
Shahrood University of Technology
By M. Norouzi
May 2021

## Slide 2: Visometric Flows & Viscometric Functions
Viscometric flows are motions that are locally equivalent to steady simple shearing motion at every particle.
Shear flow of viscoelastic fluids is anisotropic.
This anisotropic behavior objects normal stress differences.
Unlike the shear stress, the normal stresses differences are even functions of shear rate.
The viscometric functions (viscosity and coefficients of normal stress differences are mostly nonlinear functions of shear rate.

## Slide 3: Examples of Viscometric Flow

## Slide 4: Viscosity
Dependence of viscosity of three viscoelastic fluids on shear rate.

## Slide 5: Coefficients of Normal Stress Differences

## Slide 6: Normal Stress Differences
Viscometric functions of 6.8%
polyisobutylene in cetane at 24C
Ratio of N2/N1 for two polymeric Solutions.

## Slide 7: Modeling of Viscometric Functions

## Slide 8: Modeling of Viscometric Functions

## Slide 9: Effect of Temperature
Viscosity of a low density polyethylene melt versus the shear rate.
The viscosity of shear-thinning liquids has a strong dependency on temperature.

## Slide 10: Modeling the Effect of Temperature

## Slide 11: The First Normal Stress Difference

## Slide 12: The First Normal Stress Difference

## Slide 13: Shearfree Flow

## Slide 14: Shearfree Flow

## Slide 15: Some Tips on Elongational Viscosity

## Slide 16: Elongational Viscosity

## Slide 17: Elongational Viscosity

## Slide 18: Elongational Viscosity

## Slide 19: The End